## Slide 1
Top Beam (WB)
Lateral LVDT
UC
UC
Bottom Beam (UB)
Axial LVDT
Rams and Loading Plates
Insulated Sides
Thermocouples
Plasterboard Joints
Notes: Typical test setup

## Slide 2
Screw arrangement on the stud without plasterboard joint
300 mm
Notes: Linear_screw

## Slide 3
Staggered screw arrangement along the plasterboard joints
200 mm
Notes: Staggered screw arrangement

## Slide 4
Fire side plasterboard (Pb1)
open-up
Notes: T1-fireside

## Slide 5
Crack on ambient side plasterboard (Pb4)
Notes: T1-ambientside

## Slide 6
Fire side
Buckling of Stud3
Ambient side

## Slide 7
Fire side plasterboard (Pb1)
open-up
Fire side plasterboard (Pb1)
fall-off
Notes: T2-fireside

## Slide 8
Smoke patches on ambient side plasterboard (Pb4)
Discolouration of ambient side plasterboard Pb4
Notes: T2-ambientside

## Slide 9
Buckling of Stud5
Buckling of Stud4
Fire side
Ambient side
Notes: T2-buckling

## Slide 10
Partial fire side plasterboard (Pb1)
fall-off
Notes: T3-fireside

## Slide 11
No significant failure on ambient side plasterboard (Pb4)
Notes: T3-ambientside

## Slide 12
Buckling of Stud3
Fire side
Ambient side
Notes: T3-buckling

## Slide 13
Fire side plasterboard (Pb1)
open-up
Fire side plasterboard (Pb1)
fall-off
Notes: T4-fireside

## Slide 14
No significant failure on ambient side plasterboard (Pb4)
Notes: T4-ambientside

## Slide 15
Buckling of Stud2
Buckling of Stud3
Buckling of Stud4
Notes: T4-buckling

## Slide 16
Stud row -1
Stud row -2
Tracks
Glass fiber insulation
Plasterboard
Notes: T6-construction.pdf

## Slide 17
Fire side plasterboard (Pb1)
open-up
Notes: T5-fireside

## Slide 18
Crack on ambient side plasterboard (Pb4)
Notes: T5-ambientside

## Slide 19
Buckling of Stud3
Buckling of Stud4
Notes: T5-buckling

## Slide 20
Fire side plasterboard open-up
Plasterboard fall-off
Notes: T6-fireside

## Slide 21
Cracks on ambient side plasterboard (Pb4)
Notes: T6-ambient_cracks

## Slide 22
Fire side plasterboard
Burnt fire side insulation
Intact ambient side insulation
Discolouration of insulation
Notes: T6-fire side

## Slide 23
Buckling of fire side stud
Notes: T6-buckling

## Slide 24
Fire side plasterboard (Pb1)
open-up
Notes: T7-fireside

## Slide 25
Excessive bowing on ambient side plasterboard (Pb4)
Excessive contraction in LVDT
Notes: T7-ambientside

## Slide 26
Buckled fire side studs
Intact ambient side studs
Intact insulation
Notes: T7-buckling

## Slide 27
Fully calcinated fire side plasterboard Pb1, Pb2 and Pb3
Intact Pb3
Notes: T8-fireside

## Slide 28
Discolouration of ambient side plasterboard (Pb4)
Notes: T8-ambientside

## Slide 29
Buckling of all studs
Notes: T8-buckling

## Slide 30
Fire side plasterboard (Pb1) fall off. Excessive thermal bowing
Notes: T9-fireside

## Slide 31
Excessive thermal bowing and visible flame from burner
Discolouration of ambient side plasterboard (Pb4)
Notes: T9-ambientside

## Slide 32
Buckling of all studs
Notes: T9-buckling

## Slide 33
Fire side plasterboard (Pb1)
fall-off
Joint Opening
Notes: T10-fireside

## Slide 34
Crack on ambient plasterboard (Pb4)
Crack on ambient plasterboard (Pb4) joint
Notes: T10-ambientside

## Slide 35
Notes: Furnace-controller

## Slide 37
Plasterboard
Track
Track
Nogging
Nogging
Studs-Row-1
Studs-Row-2
Notes: T1-construction-connection